## Slide 1
Abaqus training
Commonly Used Material Models in Abaqus
Keng-Wit Lim
Senior Staff II
Date

## Slide 2: Why Training?
Train staff so that they can perform and use FE more effectively and intelligently, not just being “node pushers”.
Level 0 “Innovation” – focus on the fundamentals; it helps a long way.

## Slide 3: Abaqus Training Materials
Elementary tutorials on GitHub:
https://github.com/kengwitSGH/AbaqusTraining
  Currently, we have 5 tutorials. Will develop more as time goes.
Intermediate (this presentation)
Advanced (in development)
Find way to migrate to SGH internal server (GitLab)

## Slide 4: Elementary Tutorials on GitHub
Folders containing tutorial and associated input files

## Slide 5: Elementary Tutorials on GitHub (cont’d)
General information
Lesson content

## Slide 6: Elementary Tutorials on GitHub (cont’d)
Small examples (single to a few elements) to test features commonly used at SGH

## Slide 7: Elementary Tutorials on GitHub (cont’d)
Some checking or verification

## Slide 8: Elementary Tutorials on GitHub (cont’d)
Exercises
Additional notes
Links to comments (on Milo)

## Slide 9: Goal of Today’s Training
This training – perform single element tests to test material response under triaxial stress states.

## Slide 10: Performing elemental tests
Why are elemental tests important?
  Gives insight into material response
  See main features of material model
  See how parameters affect response
  Helps with interpretation of test data

## Slide 11: Performing elemental tests
  Uncover limitations of a material model (VERY IMPORTANT)
You take the red pill—Your material model may be the weakest link and your model may have no predictive power at all.
You take the blue pill—you keep making the most complicated-looking model (meshwise) and believe whatever you want to believe.

## Slide 12: Performing elemental tests
  Provides a quantitative framework to discuss material response:
    Avoid making weak analogies to pseudo, imaginary materials (“nonlinear”), which is grossly inaccurate
    Qualitative terms (“nonlinear”, “soft”, “weak”, etc.) are meaningless
“Nonlinear”
  - Not a straight line
  - I don’t know what it is, and you don’t know too
John Doyle, Professor of Control and Dynamical Systems Electrical Engineering, and BioEngineering, Caltech

## Slide 13: Triaxial stress state
Common test used for probing stress-strain response in:
  Metals
  Soil
  Concrete
Provides a homogeneous stress-state for elemental response (before failure)
Not the only possible stress-state

## Slide 14: Side: Inhomogeneous Stress State
1
2
3
4
As the neck shrinks, the nonuniform geometry alters the uniaxial stress state to a complex one involving shear components as well as normal stresses.
Post-peak test data are not supposed to be used as input into a FE model

## Slide 15: Triaxial stress state (cont’d)
Principal stresses are:
Vertical stress (varying)
Lateral stress (zero for uniaxial tests)

## Slide 16: Triaxial stress state (cont’d)
Triaxial compression (TXC)
Initial confinement
Triaxial Shearing

## Slide 17: Triaxial stress state (cont’d)
Triaxial extension (TXC) (think “squeezing”)
Initial confinement
Triaxial Shearing

## Slide 18: Triaxial stress state (cont’d)
Uniaxial

## Slide 19: Triaxial stress state (cont’d)
Shear stress (stress difference)
Pressure (mean stress)

## Slide 20: Triaxial stress state (cont’d)
Triaxial compression

## Slide 21: Commonly Used Material Models at SGH
Commonly used models:
  Metal plasticity (e.g., von Mises plasticity)
  Concrete (e.g., Concrete Damage Model)
  Soil, granular media (e.g., Drucker-Prager, Mohr-Coulomb)
Rate-independent model
Elastic-plastic materials
Quasi-static applications and monotonic loading (models are derived from tests)
For dynamics, ask others

## Slide 22: Metal Plasticity

## Slide 23: Metal Plasticity
Yield function
Isotropic (linear) hardening
Hardening modulus
Initial yield stress
Yield depends on only shear; no pressure-dependency

## Slide 24: Metal Plasticity
Uniaxial stress
Pressure
Deviatoric stress
Shear stress
If material is yielding,

## Slide 25: Metal Plasticity
Numerical example (Lesson 5 on GitHub)
Loading protocol:
Initial confinement
Triaxial Shearing

## Slide 26: Drucker-Prager

## Slide 27: Drucker-Prager
Prototypical “granular” or “soil” model. Simplest pressure-dependent material.
Yield function
Isotropic hardening

## Slide 28: Concrete

## Slide 29: Concrete
Yield function
Isotropic hardening